Large enhancement of the GMI effect in multi- ferromagnetic ribbons

Hoa N.Q., Thanh P.Q., Yu S.-C., Chau N., Gam D.T.H.

BK21 Physics Program, Department of Physics, Chungbuk National University, Cheongju 361-763; Center

for Materials Science, College of Science, Vietnam National University, Hanoi, Vietnam

Abstract: A kind of composite material consisting of stacked magnetic ribbons, each isolated with thin plastic sheets, for high-performance sensor applications. Impedance measurements were conducted in the frequency range of 1-10 MHz for a varying dc magnetic field within ?300 Oe. The giant magnetoimpedance (GMI) effect and its field sensitivity were achieved in these composite materials. The GMI effect was found increase strongly with increasing number of ferromagnetic ribbons. The GMI ratio and its field sensitivity reached the highest values of 220 % and 25 %/Oe for the composite containing five ribbons, which indicates that  the  newly  developed  composite  material  is  very  promising  for  high-performance  GMI  sensor applications. The increase in the GMI effect in the composite sample was shown to be attributable to a decrease in the electrical resistance and the increase of effective permeability.

Author Keywords: Ferromagnetic ribbon; GMI sensor; Magnetoimpedance effect

Year: 2009

Source title: Journal of the Korean Physical Society

Volume: 54

Issue: 6

Page : 2349-2352

Link: Scorpus Link

Correspondence Address: Yu, S.-C.; BK21 Physics Program, Department of Physics, Chungbuk National

University, Cheongju 361-763; email: scyu@chungbuk.ac.kr

ISSN: 3744884

DOI: 10.3938/jkps.54.2349

Language of Original Document: English

Abbreviated Source Title: Journal of the Korean Physical Society

Document Type: Article

Source: Scopus

Authors with affiliations:

1.  Hoa, N.Q., BK21 Physics Program, Department of Physics, Chungbuk National University, Cheongju 361-763

2.  Thanh, P.Q., BK21 Physics Program, Department of Physics, Chungbuk National University, Cheongju 361-763

3.  Yu, S.-C., BK21 Physics Program, Department of Physics, Chungbuk National University, Cheongju 361-763

4.  Chau, N., Center for Materials Science, College of Science, Vietnam National University, Hanoi, Vietnam

5.  Gam, D.T.H., Center for Materials Science, College of Science, Vietnam National University, Hanoi, Vietnam

References:

1.	Panina, L.V., Mohri, K., (1994) Appl. Phys. Lett, 65, p. 1189

Thank you for trying Solid Converter PDF Professional.

The trial version of this product only converts 10% of your document, with a 10 page maximum.

For this conversion, Solid Converter PDF Professional converted 1 of 2 pages.

Please purchase Solid Converter PDF Professional at http://www.solidpdf.com/buy.htm to remove this restriction.